## Slide 1
NASA soldering

## Slide 3
Tin and Lead = 60/40 solder

## Slide 4
Tin/Lead ratio/melting point

## Slide 5
Tin/Lead Fusion

## Slide 6
63/37 Eutectic solder liquid temperature

## Slide 7
60/40 solder with solid/plastic/liquid temperatures

## Slide 12
Small tip takes longer to heat the parts to the melting temperature

## Slide 13
Larger tip takes less time to heat the same part to the melting temperature

## Slide 14
Proper sized tip

## Slide 16
Discoloration burn to insulation -­‐ Accept

## Slide 17
Cut or nicked leads or wires -­‐ Reject

## Slide 19
Preferred tinning of stranded wire with heat sink -­‐ Accept

## Slide 21
Minimum insulation clearance -­‐ Accept

## Slide 22
Preferred insulation clearance -­‐ Accept

## Slide 23
Disturbed/Fractured connection -­‐ Reject

## Slide 26
Axial component mounting -­‐ Accept

## Slide 27
Axial component not seated against board -­‐ Reject

## Slide 29
Blowhole -­‐ Reject

## Slide 30
Preferred solder -­‐ Accept

## Slide 31
Minimum solder -­‐ Accept

## Slide 32
Excessive solder -­‐ Reject

## Slide 33
Lifed pad -­‐ Reject

## Slide 35
Clinched lead -­‐ Accept

## Slide 36
Cold solder, non weQng -­‐ Reject

## Slide 37
Minimum solder (should cover pad) -­‐ Accept

## Slide 38
Grainy -­‐ Reject

## Slide 39
Disturbed solder -­‐ Reject

## Slide 40
Overheated -­‐ Reject

## Slide 41
Rosin -­‐ Reject

## Slide 42
Lifed pad -­‐ Reject

## Slide 44
T05 transistor component mounting -­‐ Accept

## Slide 45
Reversed polarity -­‐ Reject

## Slide 46
Vertical mounted axial lead component -­‐ Accept

## Slide 48
Solder bridge between leads -­‐ Reject

## Slide 49
Solder bridge between leads -­‐ Reject

## Slide 50
Solder splashes/splaaers/balls -­‐ Reject

## Slide 51
Pin hole -­‐ Reject

## Slide 52
Solder spikes, peaks and icicles -­‐ Reject

## Slide 53
Stress lines -­‐ Reject

## Slide 56
Preferred mounting -­‐ Accept

## Slide 57
Toe up/curl -­‐ Reject

## Slide 58
Scratches on pads -­‐ Reject

## Slide 59
Vertical component mounting -­‐ Accept